SECTION 09 97 23 — Concrete and Masonry Coatings

Architectural Coatings and Finishes for Masonry

PART 1 - GENERAL

- SECTION INCLUDES

  - Supply and installation of base coat, reinforcing mesh and finish installed over Masonry.

- RELATED SECTIONS

  - Section 03 00 00 - Concrete

  - Section 07 90 00 - Joint Protection

  - Section 08 50 00 - Windows

- REFERENCES

  - ASTM C578 	Specification for Preformed, Cellular Polystyrene Thermal Insulation

  - ASTM C847 	Standard Specification for Metal Lath

  - ASTM C897 	Standard Specification for Aggregate for Job-Mixed Portland Cement-Based Plaster

  - ASTM B117	Test Method for Salt Spray (Fog) Testing.

  - ASTM D2247	Practice for Testing Water Resistance of Coatings in 100 Percent Relative Humidity.

  - ASTM E84 	Test Method for Surface Burning Characteristics of Building Materials.

  - ASTM E331  	Test Method for Water Penetration by Uniform Static Air Pressure Difference.

  - ASTM E695  	Method for Measuring Relative Resistance to Impact Loading.

  - ASTM E2485  	Standard Test Method for Freeze/Thaw Resistance of Exterior Insulation and Finish Systems (EIFS) and Water Resistive Barrier Coatings

  - ASTM E2486	Standard Test Method for Impact Resistance of Class PB and PI Exterior Insulation and Finish Systems (EIFS)

  - ASTM G155	Accelerated Weathering for Exposure of Nonmetallic Materials.

- ASSEMBLY DESCRIPTION

  - An exterior coating system consisting of Base Coat with embedded Reinforcing Fabric Mesh, Primer (Optional), and Finish Coat.

- SUBMITTALS

  - General: Submit Samples, Evaluation Reports and manufacturer’s product data sheets in accordance with Division 1 General Requirements Submittal Section.

  - Samples: Submit samples for approval. Samples shall be of materials specified and of suitable size as required to accurately represent each color and texture  used on project. Prepare each sample using same tools and techniques for actual project application. Maintain and make available, at job site, approved samples.

  - Manufacturer's Warranty: Submit sample copies of Manufacturer's Warranty indicating Single Source Responsibility for stucco assembly materials.

- QUALITY ASSURANCE

  - Qualifications:

    - Manufacturer: Shall have marketed stucco assemblies in United States for at least ten years and shall have completed projects of same general scope and complexity.

    - Applicator: Shall be experienced and competent in installation of stucco materials, and shall provide evidence of a minimum of five years experience in work similar to that required by this section.

    - Products manufactured under ISO 9001:2000 Quality System.

  - Architectural Coatings and Finishes for Masonry Functional Criteria:

    - General:

      - Inclined surfaces shall follow the guidelines listed below:

        - Minimum slope: 6 in (152 mm) of vertical rise in 12 in (305 mm) of horizontal run.

        - For sloped surfaces, run of slope shall be a maximum of 12 in (305 mm).

        - Usage not meeting above criteria shall be approved by Parex USA prior to installation.

      - Flashing:  Flashing shall be continuous and watertight.  Flashing shall be designed and installed to prevent water infiltration behind the Parex Architectural Coatings and Finishes for Masonry.  Refer to Division 7 Flashing section for specified flashing materials.

      - Expansion joints:  Continuous expansion joints shall be installed per contract documents

      - Building code conformance:  The construction shall be acceptable for use under the building code in force in the jurisdiction of the project.

    - Performance Requirements: Shall meet the testing requirements of the Product Performance Sheet.

- DELIVERY, STORAGE, AND HANDLING

  - Delivery: Deliver assembly materials in original packaging with manufacturer's identification.

  - Storage: Store assembly materials in a dry location, out of direct sunlight, off the ground, and protected from moisture.

- PROJECT / SITE CONDITIONS

  - Substrate Temperature: Do not apply stucco assembly materials to substrates whose temperature are below 40F (4C) or contain frost or ice.

  - Inclement Weather: Do not apply stucco assembly materials during inclement weather, unless appropriate protection is employed.

  - Sunlight Exposure: Avoid, when possible, installation of the stucco assembly materials in direct sunlight. Application of finishes in direct sunlight in hot weather may adversely affect aesthetics.

  - Do not apply stucco base coats or finishes if ambient temperature falls below 40ºF (4ºC) within 24 hours of application. Protect stucco materials from uneven and excessive evaporation during dry weather and strong blasts of dry air.

  - Prior to installation, the substrate shall be inspected for surface contamination, or other conditions that may adversely affect the performance of the stucco assembly materials, and shall be free of residual moisture.

- COORDINATION AND SCHEDULING:

  - Coordination: Coordinate Architectural Coatings and Finishes installation with other construction operations.

- WARRANTY

  - Warranty: Upon request, at completion of installation, provide manufacturer’s Standard Limited Warranty.

PART 2 - PRODUCTS

- MANUFACTURERS

  - Manufacturer, Basis of Design: Parex USA, Inc., 4125 E. La Palma Ave., Suite 250,  Anaheim, CA 92807 Contact: Architectural Sales (866.516.0061) or Technical Support (800.226.2424).

  - Components: Obtain components manufactured by Parex USA of LaHabra Fastwall 300 Stucco Assembly from authorized distributors. No substitutions or additions of other materials are permitted without prior written permission from Parex USA for this project

- MATERIALS

  - Base Coats:

    - Parex USA WeatherDry:  Waterproofing Base Coat. Acrylic co-polymer base. Requires the addition of portland cement.

    - 121 Base Coat: 100% acrylic polymer base, requiring the addition of portland cement.

    - 121 Dry Base Coat: Copolymer based, factory blend of cement and proprietary ingredients requiring addition of water.

    - 121 Optimum Base Coat: Copolymer based, factory blend of cement and proprietary ingredients requiring addition of water.

EDITOR NOTE: REINFORCING MESH IS USED FOR GAUGING THE THICKNESS OF THE BASE COAT AND IS REQURIED WITH PAREX USA WEATHERDRY

  - Reinforcing Mesh

            - 355 Standard Mesh: Weight 4.5 oz. per sq. yd. (153 g/sq m); coated for protection against alkali. Standard reinforcement of Parex EIFS, or for use with High Impact 358.14 Mesh, or Ultra High Impact 358.20 Mesh.

  - Primers

    - Parex USA Primer: 100% acrylic based coating to prepare surfaces for Parex finishes.

    - Variance VariPrime Sanded: 100% acrylic based coating to prepare surface for Cerastone and Spraystone finishes.

EDITOR NOTE: MODIFY BELOW TO SUIT REQUIREMENTS. CHOOSE ONE FINISH TYPE, TEXTURE, & COLOR WITH ACCESSORY MATERIALS TO CREATE DESIRED EFFECT

  - Finish:

    - Parex DPR Optimum Finish: Factory blended, 100% acrylic polymer based finish, integrally colored. Finish type, texture and color as selected by Architect.Finish type, texture and color as selected by Architect

    - Parex DPR Standard Finish: Factory blended, 100% acrylic polymer based finish, integrally colored. Finish type, texture and color as selected by Architect.Finish type, texture and color as selected by Architect.

    - Parex USA Variance Finish [enter selected product]: Acrylic-based specialty finish.  Finish type, texture and color as selected by Project Designer.

      - LaHabra Color Pack: factory blended, powdered oxide pigment blend for use with decorative coating compounds. Use as recommended by decking manufacturer to achieve desired finish.

      - Variance Antiquing Gel: a water-based, tinted, semi-transparent, acrylic emulsion for staining, sealing, and protecting concrete, masonry and other cementitious substrates.  Use as required to achieve desired finish.

      - Variance VariSeal is a 100% acrylic, water based sealer. Improves scratch and scuff resistance and adds depth of color.

EDITOR NOTE: ADD CLEAR SEALER WHERE ENHANCED CLEANABILTY IS DESIRED FOR HIGH SOILING EXPOSURES.

    - Parex USA Clear Sealer: 100% acrylic, transparent, permeable, dirt resistant sealer for use as a protective coating over acrylic finishes. Use 600 Clear or 610 Matte Clear as detailed on drawings.

  - Water: Clean, potable water

  - Portland Cement: ASTM C150, Type I or Type I-II.

- RELATED MATERIALS AND ACCESSORIES

  - Substrate Materials:

    - Concrete Masonry Units (CMU): Non-painted (uncoated).

    - Concrete (poured or pre-cast).

    - Unglazed brick and masonry units.

    - Other Approved by Parex USA in writing prior to the project

  - Flashing: Refer to Division 7 Flashing Section for flashing materials.

  - Sealant System:

    - Sealants shall conform to ASTM C 920, Grade NS.

    - Expansion joints between sections of Parex EIFS shall have a minimum width of 3/4 in (19 mm).

    - Sealant backer rod shall be closed-cell polyethylene foam.

    - Apply sealant to tracks or base coat of Parex EIFS.

    - Refer to Parex USA current bulletin for listing of sealants which have been tested and have been found to be compatible with Parex EIFS.

    - Color shall be as selected by Architect.

    - Joint design, surface preparation, and sealant primer shall be based on sealant manufacturer's recommendations and project conditions.

EDITOR NOTE: PART 3 EXECUTION BELOW INVOLVES ONSITE WORK AND SHOULD INCLUDE PROVISIONS FOR INCORPORATING MATERIALS AND PRODUCTS INTO PROJECT. TYPICALLY, "CONDITIONS OF THE CONTRACT" ESTABLISH RESPONSIBILITY FOR "MEANS, METHODS, TECHNIQUES, AND SAFETY” REQUIREMENTS OF CONSTRUCTION WITH CONTRACTOR. SPECIFICATIONS SHOULD AVOID CONFLICTS WITH THIS CONTRACTUAL PRINCIPLE.

PART 3 - EXECUTION

- EXAMINATION

  - Verify project site conditions under provisions of Section 01 00 00.

  - Compliance: Comply with manufacturer's instructions for installation of coatings.

C.	Substrate Examination: Examine prior to Parex Base Coat installation as follows:

    - Substrate shall be free of dust, dirt, laitance, efflorescence, and other harmful contaminants.

    - Substrate construction in accordance with substrate material manufacturer's specifications and applicable building codes.

    - Substrate shall be cured concrete (28 days minimum)

    - Substrate shall have no irregularities greater than 1/4" (6.4 mm), and shall be sound and free of foreign substances, including paint, bond breakers, form oils, laitance, scaling and flaking.

    - Unsatisfactory conditions shall be corrected before the application of the coatings.

    - Painted surfaces shall have paint removed to achieve a substrate with 90% or more of the surface free of paint.

    - Sanding surfaces shall be eliminated mechanically, then washed with clear water.

    - Remove efflorescence using mechanical removal and/or a diluted acid solution followed by complete rinsing.

    - Concrete surfaces shall be level and free of voids over 1/8" (3 mm) across. Glossy surfaces shall be dulled by chemical or mechanical means. Thoroughly remove all residues.

  - Advise Contractor of discrepancies preventing installation of the Parex Architectural Coatings and Finishes.   Do not proceed with the Parex Architectural Coatings and Finishes work until unsatisfactory conditions are corrected.

- PREPARATION

  - Protection: Protect surrounding material surfaces and areas during installation of system.

  - Clean surfaces thoroughly prior to installation.

  - Prepare surfaces using the methods recommended by the Manufacturer for achieving the best result for the substrate under the project conditions.

- MIXING

  - Mix proprietary products in accordance with Manufacturer's instructions.

- APPLICATION

  - General: Installation shall conform to this specification and Parex written instructions and drawing details.

  - Base coat

    - If leveling is required, apply any Parex 121 Base Coat.  Parex 121 Base Coat may be applied up to 3/8" (9.5 mm) and 121 Dry up to 1/2 in. (13 mm) thick in a single pass when used as a leveler.

    - Apply base coat and fully embed mesh if applicble in base coat.

  - Bond supplemental EPS shapes as indicated on the drawings.  Bond shapes to EPS or to dry reinforced base coat using any Parex 121 Base Coat & Adhesive as an adhesive.  Allow 24 hours to dry.  Refer to Parex Standard System Specification for materials and installation of Base Coat and Mesh over EPS shapes.

  - Apply primer to base coat after drying. Primer may be omitted if it is not required by the Manufacturer's product data sheets for the specified finish coat or otherwise specified for the project.

  - Finish Coat: Apply finish coat to match specified finish type, texture, and color. Do not apply finish coat to surfaces to receive sealant. Keep finish out of sealant joint gaps.

- CLEAN-UP

  - Removal: Remove and legally dispose of Parex Architectural Coatings and Finishes for Masonry  component debris material from job site.

  - Clean EIFS surfaces and work area of foreign materials resulting from EIFS operations.

- PROTECTION

  - Provide protection of installed materials from water infiltration into or behind them.

  - Provide protection of installed stucco from dust, dirt, precipitation, and freezing during installation.

  - Provide protection of installed finish from dust, dirt, precipitation, freezing and continuous high humidity until fully cured and dry.

  - Clean exposed surfaces using materials and methods recommended by the manufacturer of the material or product being cleaned. Remove and replace work that cannot be cleaned to the satisfaction of the Architect/Owner.

END OF SECTION									    Rev.  January 2013

Disclaimer: This guide specification is intended for use by a qualified designer. The guide specification is not intended to be used verbatim as an actual specification without appropriate modifications for the specific use intended. The guide specification must be integrated into and coordinated with the procedures of each design firm, and the requirements of a specific project.  For additional assistance, contact Parex USA’s Architectural Sales (866.516.0061) or Technical Support (800-226-2424).

Product Performance Sheet | Page 1

Architectural Coatings and Finishes

| Fire Performance | Method | ICC or ASTM Criteria | Results |
| --- | --- | --- | --- |
| Surface Burning Characteristic | ASTM E84 | Individual components shall each have a flame spread <25, and smoke developed < 450 | Flame Spread: 0 to 15 Smoke Developed: 0 to 15 |

| EIFS Strength | Method | ICC or ASTM Criteria | Results |
| --- | --- | --- | --- |
| Flexural Strength | ASTM C203 | No Requirement | 60.6 psi (418 kPa) |
| Falling Ball Impact | ASTM D1037 | No Requirement | 92 to over 600 in-lbs |
| Creep Resistance of Adhesive | ASTM D2294 | No Requirement | 28 days 208 psf shear stress: no creep |
| Tensile Bond Strength | ASTM E2134 | Minimum 15 psi (103kPa) | Pass |

| Environmental Durability | Method | ICC or ASTM Criteria | Results |
| --- | --- | --- | --- |
| Abrasion Resistance | ASTM D968 | No cracking or loss of film at 528 quarts (500 L) of sand | Pass: 500 Liters |
| Accelerated Weathering | ASTM G153/ (ASTM G23) ASTM G154 | No deleterious effects* at 2000 hours when viewed under 5x magnification | Pass: 2000 Hours |
| Freeze/Thaw Resistance | ASTM E 2485 | No deleterious effects* at 10 cycles when viewed under 5x magnification | Pass: 60 cycles |
| Fungus Resistance | MIL STD 810B | No Requirement | Pass: 28 days- no growth |
| Mildew Resistance | ASTM D3273 | No growth supported during 28 day exposure period | Pass |
| Water Penetration | ASTM E331 | No water penetration beyond the plane of the base coat/EPS board interface after 15 minutes at 6.24 psf (299 Pa) | Pass |
| Moisture Resistance | ASTM D2247 | No deleterious effects at 14 day exposure | Pass |
| Salt Fog Resistance | ASTM B117 | No deleterious effects* at 300 hours | Pass: 500 hours |
| Wind Driven Rain | F.S. TT-C-555B | No Requirement | Pass: 24 hours |

*No deleterious effects: no cracking, checking, crazing, erosion, rusting, blistering.

Where several tests on different materials are summarized, a range of values is shown.  This summary has been prepared to provide quick but partial information on how certain combinations of Parex products perform during certain tests.  It is not a complete description of the test procedures or of the results thereof. Copies of original test reports are available at no charge upon request.  Please contact Parex USA’s Architectural Sales (866-516-0061) or Technical Support Department (800-226-2424) if further information is required.